## Slide 1: Analog Electronics Fundamentals 105
-DIY PCB Etching

## Slide 2: 1 DIY PCB Etching
Before we get started, do yourself a favour and read these safety tips:
  When dealing with caustic chemicals, please wear appropriate protection (Protective Eyewear, Rubber Gloves)
  Handle chemicals in a well ventilated area
  Use Caution
  Don’t be an idiot!
Etching Solution Recipe:
  In a non metallic container, pour 2 cups of Hydrogen Peroxide (3%).
  Slowly, pour 1 cup of muriatic acid into the Hydrogen Peroxide.
  1 pinch of Kosher salt (this will speed up the etching process).
Transferring board layouts to Copper Clad PCB:
  Vigorously clean your copper board with Steel wool and dry. (Do not touch with fingers).
  Print your board layout on a sheet of glossy paper (you can use old magazines/catalogs).
  Cut the glossy paper to the size of your board layout, but leave some excess to handle.
  Put the printed layout face down on copper board, and put a sheet of normal paper on top.
  With your clothes iron set on the hottest setting (Cotton), apply heat and a lot of pressure, without moving, for 2 minutes.
  Motion the iron around on the board for 5 minutes.
  When the board has cooled, put it in a bath of water.
  Wait a few minutes for the paper to start dissolving, and gently peel the paper away.
Etching Process
  Put your board in the etching solution, face up. It should take about 30 minutes to etch properly. Keep an eye on it, to not over etch.
  In the final minutes of the etching process, swirl the container a little, that will help etching in tight spots.